SECTION 096566 - SYNTHETIC ATHLETIC FLOORING

PART 1 - GENERAL

- DESCRIPTION

- Related work specified under other sections.

- CONCRETE SUBFLOORS - SECTION 03300

- Slab Depression: Equal to thickness of selected flooring.

- Concrete Finish: Shall be steel troweled, dense and finished smooth, not polished.

- Slab Tolerance:  A tolerance of 1/8" (3mm) in 10' (3m) radius shall be maintained throughout. Floor Flatness and Floor Levelness (FF and FL) numbers are not recognized.

- No concrete curing, hardening or sealing agents shall be applied to the concrete subfloor.

- MEMBRANE WATERPROOFING - SECTION 07100

- Concrete subfloors on or below grade shall be adequately waterproofed, beneath, at perimeter walls, and on earth side of below grade walls.

- Type and extent of membrane shall be determined by the Project Engineer and installed by the General Contractor.

- THRESHOLDS - SECTION 08700

  - REFERENCES:

American Society for Testing & Materials

- ASTM C 501:  Standard Test Method for Relative Resistance to Wear of Unglazed Ceramic Tile by the Taber Abraser

- ASTM C 518:  Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus

- ASTM D 395:  Standard Test Method for Rubber Property – Compression Set

- ASTM D 412: Standard Test Method for Tension Testing for Rubber and Elastomers

- ASTM D 624:  Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers

- ASTM D 1149:  Standard Test Methods for Rubber Deterioration – Cracking in an Ozone Controlled Environment

- ASTM D 1894-01: Standard Test Method of Static and Kinetic Coefficients of Friction of Plastic Film and Sheeting.

- ASTM D 2047: Standard Test Method for Static Coefficient of Friction of Floor Surfaces

- ASTM D 2240:  Standard Test Method for Rubber Property—Durometer Hardness

- ASTM E 423:  Standard Test Method for Normal Spectral Emittance at Elevated Temperatures of Non-conducting Specimens

- ASTM F 925:  Standard Test Method for Resistance to Chemicals of Resilient Flooring

- ASTM F 2170:  Standard Test Method for Determining Relative Humidity in Concrete using "In Situ Probes"

  - SUBMITTALS

- Submit Connor Sports ElastiRoll/ElastiMat/ElastiLock™ specification sheets.

- Sample - Submit one sample of specified system, if requested by Architect.

- Maintenance Literature - Upon completion of floor installation, send a Connor Sports Recycled Rubber Care & Maintenance Guide to owner, attendants or individuals in charge and responsible for the upkeep of the building. These instructions shall be followed. Any variations, deviations or substitutions shall be submitted to Connor Sports for approval.

  - QUALITY ASSURANCE

- MANUFACTURER: Manufacturer of resilient flooring shall be a firm specializing in manufacturing products specified in this section.

- INSTALLER:

- The complete installation of the flooring system, as described in the scope of these specifications, shall be carried out by an experienced installer (Flooring Contractor), and the work shall be performed in accordance with most recent installation instructions of the manufacturer.

- Installer (Flooring Contractor) shall be liable for all matters related to installation for a period of one year after the floor has been substantially installed and completed.

  - WORKING CONDITIONS

  - Synthetic materials specified herein shall not be installed until all masonry, painting, plaster, tile, marble and terrazzo work is completed, and overhead mechanical trades and painters have finished in the synthetic floor areas. The building shall be enclosed and weather tight.

  - Permanent heat, light and ventilation shall be installed and operating during and after installation. Subfloors shall be clean, dry and free from dirt, dust, oil, grease, paint, and alkali, concrete curing agents, hardening and parting compounds, old adhesive residue or other foreign materials. The general contractor shall provide an area where the stored materials can be maintained at a minimum of 55°F (12.8 °C) and under 50% relative humidity. Ideal installation and storage conditions are the same as those which will prevail when building is occupied. Moderate room temperature of 65°F to 80°F (18.3°C to 26.7°C) or more shall be maintained for a week prior to, during and for 72 hours after installation.

  - Flooring installation shall not begin until all sub-contract work which would cause damage, dirt, dust or interruption of normal installation pace is completed. The installation area shall be closed to all traffic and activity for a period to be set by the flooring contractor.

  - Moisture vapor transmission of the concrete slab must not exceed 85% RH as per ASTM F2170.

  - Environmental Limitations

- Comply with requirements of athletic flooring material supplier's requirements.

- Adhere to all MSDS requirements for materials employed in the work. Protect all persons from exposure to hazardous materials.

  - After synthetic floors are installed, area to be kept locked by general contractor to allow curing time for system. No other trades or personnel are allowed on floor until accepted by owner.

  - WARRANTY

- Connor Sports warrants that the materials it has supplied will be free from manufacturing defects for a period of one (1) year. The foregoing warranty is in lieu of and excludes all other warranties not expressly set forth herein, whether expressed or implied in operation of law or otherwise, including, but not limited to, any implied warranties of merchantability or fitness. This warranty is expressly limited to the flooring materials (goods) supplied by Connor Sports. This warranty does not cover floor damage caused (wholly or in part) by fire, winds, floods, moisture, other unfavorable atmospheric conditions or chemical action, nor does it apply to damage caused by ordinary wear, misuse, abuse, negligent or intentional misconduct, aging, faulty building construction, concrete slab separation, faulty or unsuitable subsurface or site preparation, settlement of the building walls or faulty or unprofessional installation of Connor Sports flooring systems.

- Connor Sports shall not be liable for incidental or consequential losses, damages or expenses directly or indirectly arising from the sale, handling or use of the materials (goods) or from any other cause relating thereto, and their liability hereunder in any case is expressly limited to the replacement of materials (goods) not complying with this agreement or, at their election, to the repayment of, or crediting buyer with, an amount not to exceed the purchase price of such materials (goods), whether such claims are for breach of warranty or negligence. Any claim shall be deemed waived by buyer unless submitted to Connor Sports in writing within 30 days from the date buyer discovered, or should have discovered any claimed breach.

PART 2 - PRODUCTS

2.1	MATERIALS

- ElastiRoll/ElastiMat/ElastiLock™ – Flooring consisting of polymeric bound VULCANIZED recycled rubber mixed with EPDM granules.

- Colors – select from standard colors (refer to brochure).

- Physical Properties

- Hardness – Shore A  (ASTM D-2240). . . . . . . . . . . . . . . . . . . . .. . . . . . . . . . . . . . . . . . . . . . 60 +/- 5

- Taber Abrasion  (ASTM C-501 – 1kb wt. 7000 cycles) . . . . . . . . . . . . . .  . . . .. . . . . . . . . . . 6% wt. loss

- Compression Set  (ASTM D-395 method B) . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . 36% max

- Tensile Strength  (ASTM D-412) . . . . . . . . . . . . . . . . . . . . .. . . . . . . . . . . . .. . . . . . . . . . . . . 300 min PSI

- Elongation  (ASTM D-412) . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . .. . . . . . . . . . . . . . . . 75% min

- Chemical Resistance  (ASTM F-925) . . . . . . . . . . . . . . . . . . . . . . .  . . . . . . . . . . . . . . . . . . . .No change

- Acoustic Properties    (ASTM E-423) . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . .NRC = 0.10

- Thermal Conductivity, BTU-in/hr-ft2-°F (ASTM C518): . . . . . ..  . . . .. . . . . . .  . . .. .. . . .   approx. 0.406

- Weight . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . .. . . . . . . . . . 2 lb/ft2

- Tear Resistance   (ASTM D-624) . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . 80 PLI

- Coefficient of Friction   (ASTM D-2047) . . . . . . . . . . . . . . . . . . .. . . . . . . . . . . . . . . . . . . . . . 0.9 min, Wet or Dry

- Ozone Resistance   (ASTM D-1149-50 pphm)

- (70 hours @ 104˚ F) . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . No effect

- Sizes

- ElastiRoll™ – 4’ x 15’ to 50’ (1.22m x 4.6m to 15.2m)

- ElastiMat™ – 24” x 24” (0.6m x 0.6m)

- ElastiLockTM – 28.5” x 28.5” (0.7m x 0.7m)

- Thickness – 3/8” (9.5mm) (8mm optional)

- ElastiRoll/ElastiMat™ Adhesive – One-component urethane as supplied by Connor Sports.

- 1.	Optional Adhesive (specify or delete) – Two-component epoxy for questionable substrates as directed.

- E.    Optional Base (specify or delete) - Vinyl wall base 4" high; select from supplier standard colors.

PART 3 - EXECUTION

3.1  	INSPECTION

- Inspect concrete slab for proper tolerance and dryness. Test moisture vapor transmission of concrete flooring by means of in-situ probes per ASTM F2170, results not to exceed 85%. Report any discrepancies to general contractor.

- Concrete slab shall be broom cleaned by general contractor.

- Installer (Flooring Contractor) shall approve and document all working conditions provided in General Specifications prior to commencement of installation.

3.2 	INSTALLATION

- ElastiRoll™

  - Unroll ElastiRoll™ and allow it to relax. Do not cut to final dimensions until laid into adhesive.

  - Thoroughly mix the one-component urethane adhesive and apply directly to the concrete subfloor with a notched trowel per manufacturer’s instructions.

  - Install ElastiRoll™ into freshly applied adhesive wall to wall, scribing and fitting neatly at walls, around columns, and around door frames. Do not allow compression fit at any seams. Roll with medium size roller. When floor is complete, roll again.

  - Wipe adhesive that oozes between seams with recommended solvent.

- ElastiMat™

  - Square the room or area to be installed.

  - Mark the floor off in quarters.

  - Thoroughly mix the one-component urethane adhesive and apply directly to the concrete subfloor with notched trowel per manufacturer’s instructions.

  - Place tile firmly into adhesive and butt the adjacent tiles.

  - Lay the tile in straight tile pattern or broken joint pattern.

  - Only apply as much adhesive as can be covered in 20 minutes.

  - Roll with medium size roller. When floor is complete, roll again.

  - Wipe adhesive that oozes between seams with recommended solvent.

- ElastiLockTM

- Square the room or area to be installed.

- Mark the floor off in quarters.

- Place tile firmly into puzzle locks of adjacent tiles.

- Lay the tile in straight tile pattern.

- Follow arrows on tiles to be sure all are laid the same direction.

- Wall base (optional) – Install vinyl base anchored to walls with base cement.

- Remove all excess and waste materials from the area of work.  Dispose of empty containers in accordance with federal and local statutes.

END OF SECTION 096566